# The desulphurization model by Arcelor Eisenhüttenstadt

Andreas Pudack

- Hot metal desulphurization structure

The hot metal desulphurization plant built by Krupp Polysius was completely modernized by SMS Mevac in 2000/2001. There are two separate stands, which are equipped for exhausting and slag removal.

Lime, carbide and magnesium are used as the desulphurization agents. The structure of the desulphurization is shown in figure 1:

Figure 1

The desulphurization agents are conveyed separately into the silo by dry nitrogen. The high reactive burnt lime is produced in an own limestone burning and grinding plant.  Magnesium and Carbide is imported by tanks on railway or trucks. To the fluidization of lime a silicon oil is used. It is added into the lime mixer in a ratio of approximately 1l to 1000 kg. The filling of the pneumatic delivery system is done gravimetrical. Because of the permanent dispersion in the delivery system we have good conditions for the conveyance of the desulphurization agents. The most important thing for the consistent charging of the desulphurization agents and the reaction are stable pressure conditions. This is also the condition for a long performance of the injection lances. Figure 2 show’s the layout of charging the desulphurization agents of one line with all parameters from the pneumatic delivery system into the hot metal. During the blowing process the conveying pressure is 4,5 bar and the delivery pressure is between 3,7 – 3,9 bar. The flow rate for the conveying gas is 27 Nm³/h.

Figure 2

- Technical data

| Heat weight | Sulphur before | Sulphur after | Temperature before | Temperature after |
| --- | --- | --- | --- | --- |
| 210 t | 0,035 % | 0,002 % | 1360 °C | 1340 °C |

The average of hot metal analysis could be given with 4,95% C, 0,35%Si, 0,27%Mn, 0,076%P.

Following injection options could be used:

- Monoinjection with lime and carbide

- Co-injection lime+Mg and carbide+Mg

- ECO- injection (in fact a co-injection carbide+Mg, in which a part of  carbide is substituted by lime in the beginning and the end)

The physical and chemical qualities of the desulphurization agents are summarized in table 1:

|  | lime | carbide | magnesium |
| --- | --- | --- | --- |
| analysis | 98% CaO | 70% CaC2 15% CaO 5% C | 97% Mg 3% Coating |
| grain size | <0,063mm 72% <0,09 mm 95% <0,63 mm 99% <1 mm 100% | <0,063mm 80% <0,09 mm 90% | 0,2-0,5mm 40-50% 0,5-0,8mm 40-50% 0,8-1 mm 5% |
| Fluidization of lime: silicon oil (0,96l / t CaO) Slag bounder for steel grades with lowest S-contents (<0,05%) |

Table 1

- The desulphurization model

The model includes several factors to determine the quantity of the desulphurization agents. Initial situation is the calculated sulphur of the hot metal analysis at the torpedo ladles before treatment and the aim sulphur content. The temperature is considered to be constant.

Basis is the calculation of the equivalent for magnesium. It describes the need for a desulphurization agent based on the efficiency of magnesium. For the desulphurization agents lime and carbide correction factors are considered to calculate the quantity. These correction factors include the dependence of temperature, the chemical quality and dependences on slag quantities. The Mg-quantities [kg/tHM] for corresponding sulphur contents are shown in table 2.

| Initial [S] in ppm | Final [S] in ppm |
| --- | --- |
|  | 20 | 50 | 100 | 200 | 300 |
| 1500 | 1,19 | 1,13 | 0,907 | 0,831 | 0,755 |
| 900 | 0,801 | 0,695 | 0,588 | 0,493 | 0,398 |
| 800 | 0,732 | 0,618 | 0,518 | 0,419 | 0,27 |
| 700 | 0,662 | 0,551 | 0,454 | 0,358 | 0,262 |
| 600 | 0,594 | 0,485 | 0,392 | 0,299 | 0,205 |
| 500 | 0,526 | 0,418 | 0,33 | 0,239 | 0,143 |
| 400 | 0,457 | 0,332 | 0,259 | 0,176 | 0,093 |
| 300 | 0,387 | 0,272 | 0,199 | 0,126 | 0 |
| 200 | 0,311 | 0,199 | 0,135 | 0 | 0 |
| 125 | 0,243 | 0,135 | 0,081 | 0 | 0 |
| 100 | 0,216 | 0,108 | 0 | 0 | 0 |
| 75 | 0,181 | 0,08 | 0 | 0 | 0 |
| 50 | 0,135 | 0 | 0 | 0 | 0 |

Another process model calculates a cost rate for all the five injection options of every heat. This cost rate depends on the prices of the desulphurization agents. For EKO the most cost-efficient methods are injections using lime. The reason for this is the own production of lime.

  - Monoinjection (lime, carbide)

The monoinjections have a constant agent flow rate of 50 kg/min. These injections are very rarely (temperature losses due to longer desulphurization time for the monoinjection with lime and highest costs with carbide). The monoinjection with lime shows the lowest specific costs for the desulphurization process. This advantage is lost at the following converter process by higher hot metal ratio or by added costs through addition of FeSi for heating.

  - Co-injection

Because of the conditions in Eisenhüttenstadt the co-injection of lime–Mg is the best desulphurization option. It is used for a sulphur difference of 350ppm. The first phase is a monoinjection of lime (60kg) with a flow rate of 50 kg/min. It follows a co-phase in which the flow rate for lime is 40kg/min and for magnesium 10kg/min. The quantity of both desulphurization agents are done by the calculating system. The last phase is a monoinjection of lime (70kg) with a flow rate of 50 kg/min.

The co-injection of carbide-Mg follows the same process like lime-Mg. The only difference is the quantity of the agents of the monophase. In this case 40 kg carbide in phase 1 and 30 kg in phase 2 are blown into the melt.

3.3.      ECO-injection

The ECO-injection is used for sulphur differences that are higher than 350ppm. In this case the desulphurization effectiveness is better and less time is needed. The ECO-injection is characterized by 5 phases. Monophase 1 is a lime injection of 70 kg with a flow rate of 50 kg/min. The next phase is a monoinjection of carbide with a quantity of 12 kg and a flow rate of 40 kg/min. The 3rd phase contains a co-injection with carbide and Mg. The fourth phase is a monophase of carbide injection with 12 kg and a flow rate of 40kg/min. The last phase is a monophase of lime injection with 40kg and a flow rate of 50kg/min.

- Economic efficiency

In the following figure 3 the specific desulphurization agent costs are represented for the desulphurization options CaO-Mg, CaC2-Mg und ECO-injection. It shows clearly, that due to the lime price (including the costs of fluidization) the co-injection CaO-Mg is the most efficient method for Eisenhüttenstadt. It is also clear, that the co-injection CaC2-Mg is the most uneconomic method. In the case of CaC2-Mg injection the specific costs are higher than in the ECO-injection although the sulphur difference is lower.

Figure 3

In contrast to existing opinions in literature the Fe losses in the slag, while using the co-injection lime-Mg, are not higher than with other injection options. Own investigations showed that the iron losses increased rapidly if the desulphurization difference is higher than 300 ppm and because of that the quantity of slag is very high. The slag quantity is shown in figure 4 and the iron losses in figure 5.

Figure 4

Figure 5

- Summary

- The accuracy of the desulphurization model by Arcelor Eisenhüttenstadt works satisfying, the post treatment rate is less than 6%.

- Due to internal conditions the Co-injection lime + Mg is used mainly. That’s why the stable fluidization of the lime is the most important criteria. A result of this is a high performance of the lances (Ø 750 min, max.1350 min).

- If there are time problems or higher [S] – differences, the ECO-injection is used.

- While practicing the addition of soda ash before the desulphurization treatment and the use of a rotation lance this year, the expected results will be decreasing iron losses in the slag and less quantities of desulphurization agents.